Supporting Information

Deep-Ultraviolet Nonlinear-Optical Crystals LiBePO4 and BeP2O6 by Ionic Potential Modulation towards Uniform Arrangement of PO4 Groups

Xia Zhang,a Jian-Qiang Shen,a Hong-Xiao Lv,b Peng-Hui Guo,a Yi-Gang Chen,*a Chun-Li Hu*c ,Xian-Ming Zhang*a,b

aKey Laboratory of Magnetic Molecules and Magnetic Information Material of Ministry of Education, School of Chemistry and Material Science, Shanxi Normal University, Taiyuan 030031, China;

bCollege of Chemistry & Chemical Engineering, Key Laboratory of Interface Science and Engineering in Advanced Material, Ministry of Education, Taiyuan University of Technology, Taiyuan, Shanxi 030024, P. R. China.

cState Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou 350002, China

Table of Contents

Table S1. Atomic coordinates and equivalent isotropic displacement parameters (Å2) for LiBePO4 and BeP2O6.

Table S2. Selected bond lengths (Å) and angles (deg) for LiBePO4 and BeP2O6.

Table S3. Applicability of ionic potential modulation strategy in known alkali/alkaline-earth metal NLO materials.

Figure S1. Crystal structures of Cs4LiBe4P7O24.

Figure S2. Simulated and experimental powder XRD patterns of LiBePO4 and BeP2O6.

Figure S3. High-resolution XPS spectra of LiBePO4 and BeP2O6.

Figure S4. TG and DSC curves of LiBePO4 and BeP2O6.

Figure S5. IR spectra of LiBePO4 and BeP2O6.

References.

Table S1. Atomic coordinates and equivalent isotropic displacement parameters (Å2) for (a) LiBePO4 and (b) BeP2O6. U(eq) is defined as one-third of the trace of the orthogonalized Uij tensor.

(a) LiBePO4

| Atom | x/a | y/b | z/c | U(eq) | BVS |
| --- | --- | --- | --- | --- | --- |
| Li1 | 3550(4) | 8010(4) | 4712(3) | 18.8(8) | 0.87 |
| Li2 | 5972(3) | 574(4) | 4711(3) | 21.2(10) | 0.81 |
| Li3 | 5740(3) | 5297(4) | 4773(3) | 15.8(8) | 0.88 |
| Li4 | 6134(3) | 1757(4) | 7247(3) | 14.5(8) | 0.96 |
| Li5 | 3160(3) | 12849(4) | 4741(3) | 16.0(8) | 0.88 |
| Li6 | 3639(3) | −767(4) | 7250(3) | 14.3(8) | 0.97 |
| Li7 | 6412(3) | 7020(4) | 7251(3) | 13.8(8) | 0.98 |
| Li8 | 8918(3) | −483(4) | 7256(3) | 16.0(8) | 0.96 |
| Be1 | 2888.8(18) | 5611(3) | 5375.6(18) | 7.7(5) | 2.07 |
| Be2 | 5441.2(18) | 629(3) | 2819.5(19) | 7.1(5) | 2.08 |
| Be3 | 5414.6(18) | −1901(3) | 5368.2(19) | 7.0(5) | 2.07 |
| Be4 | 2931.4(19) | 3114(3) | 2832.2(19) | 7.9(5) | 2.11 |
| Be5 | 5087.2(19) | 2806(3) | 5351.2(19) | 7.3(5) | 2.08 |
| Be6 | 2625.4(19) | 10273(3) | 5350.0(18) | 7.1(5) | 2.04 |
| Be7 | 5721.0(18) | 5337(3) | 2847.9(19) | 6.9(5) | 2.09 |
| Be8 | 3226.5(18) | 7853(3) | 2833.7(19) | 7.1(5) | 2.09 |
| P1 | 4470.4(3) | 321.5(6) | 5970.0(3) | 4.65(12) | 5.32 |
| P2 | 1955.5(3) | 7836.8(6) | 5972.0(3) | 4.60(12) | 5.35 |
| P3 | 4760.6(3) | 5644.0(6) | 5977.8(3) | 4.64(12) | 5.31 |
| P4 | 5107.6(3) | 7832.5(6) | 3473.0(3) | 4.27(12) | 5.33 |
| P5 | 7272.7(3) | −1876.7(6) | 5971.4(3) | 4.50(12) | 5.28 |
| P6 | 4817.5(3) | 3085.6(6) | 3461.8(3) | 4.37(12) | 5.27 |
| P7 | 2591.9(3) | 10310.0(6) | 3472.2(3) | 4.34(11) | 5.23 |
| P8 | 2330.4(3) | 5604.7(6) | 3466.8(3) | 4.37(12) | 5.40 |
| O1 | 1081.1(9) | 7456.1(15) | 6082.1(9) | 7.7(3) | 2.00 |
| O2 | 5466.5(9) | 6831.8(15) | 6106.2(9) | 7.6(3) | 2.03 |
| O3 | 3845.5(9) | 6356.4(15) | 5607.5(9) | 7.4(3) | 2.00 |
| O4 | 6363.5(9) | −1144.9(15) | 5608.2(9) | 7.6(3) | 1.99 |
| O5 | 2797.1(10) | 11946.3(15) | 3547.5(10) | 8.1(3) | 2.03 |
| O6 | 2265.4(10) | 4451.1(14) | 2747.1(9) | 7.3(3) | 2.00 |
| O7 | 3251.6(10) | 9545.6(14) | 3131.6(9) | 7.4(3) | 1.95 |
| O8 | 4368.3(10) | 1878.4(14) | 5591.3(9) | 7.4(3) | 1.97 |
| O9 | 2704.0(10) | 7763.7(16) | 6892.1(9) | 8.0(3) | 2.06 |
| O10 | 3609.0(9) | −86.7(15) | 6099.3(9) | 7.4(3) | 2.01 |
| O11 | 4768.9(10) | 1951.2(14) | 2736.0(9) | 7.4(3) | 2.01 |
| O12 | 5754.7(9) | 7040.4(14) | 3129.5(9) | 7.4(3) | 1.96 |
| O13 | 2571.0(11) | 4835.3(13) | 4382.1(10) | 7.4(3) | 1.95 |
| O14 | 7358.5(11) | −3008.2(15) | 5297.2(10) | 8.5(3) | 2.00 |
| O15 | 5228.7(10) | 248.9(15) | 6886.3(9) | 7.9(3) | 2.07 |
| O16 | 5485.6(10) | 4317.2(15) | 3564.6(10) | 8.2(3) | 1.98 |
| O17 | 5083.3(11) | 2305.8(14) | 4371.7(10) | 8.2(3) | 1.97 |
| O18 | 7982.6(9) | −698.4(14) | 6098.6(9) | 7.6(3) | 2.03 |
| O19 | 4643.4(10) | −743.9(15) | 5306.9(10) | 8.2(3) | 1.97 |
| O20 | 5183.0(11) | 7254.8(15) | 4401.8(10) | 7.9(3) | 1.98 |
| O21 | 1661.8(9) | 9948.0(14) | 2800.0(9) | 7.6(3) | 2.03 |
| O22 | 5337.2(10) | 9460.2(15) | 3556.7(10) | 8.0(3) | 1.98 |
| O23 | 1885.1(10) | 9382.8(14) | 5583.0(9) | 7.0(3) | 2.02 |
| O24 | 1419.5(9) | 6346.8(14) | 3165.4(9) | 8.3(3) | 1.93 |
| O25 | 2709.0(10) | 9730.7(14) | 4407.9(10) | 7.7(3) | 1.99 |
| O26 | 3903.6(9) | 3806.1(14) | 3159.6(9) | 8.2(3) | 1.96 |
| O27 | 3013.7(10) | 6804.2(16) | 3560.1(10) | 8.4(3) | 1.96 |
| O28 | 4850.8(10) | 4523.7(15) | 5301.9(10) | 8.8(3) | 1.99 |
| O29 | 7419.6(10) | −2589.0(16) | 6879.1(10) | 8.2(3) | 2.05 |
| O30 | 2117.2(10) | 6745.6(15) | 5321.0(10) | 8.9(3) | 1.99 |
| O31 | 4910.8(10) | 4928.4(16) | 6885.9(9) | 8.3(3) | 2.05 |
| O32 | 4174.2(9) | 7493.5(14) | 2794.1(9) | 8.2(3) | 2.00 |

(b) BeP2O6

| Atom | x/a | y/b | z/c | U(eq) | BVS |
| --- | --- | --- | --- | --- | --- |
| Be1 | 6779(7) | 388(7) | 6830(4) | 15.5(10) | 2.21 |
| Be2 | 6770(7) | 601(6) | 1799(4) | 12.0(10) | 2.22 |
| Be3 | −1171(7) | 4990(7) | 5820(4) | 15.5(11) | 2.20 |
| Be4 | 1429(7) | 10018(6) | 9147(4) | 14.6(10) | 2.20 |
| P1 | 6133.8(14) | 3024.3(13) | 3273.8(7) | 12.1(2) | 5.32 |
| P2 | 5902.1(14) | 2531.5(15) | 5353.0(7) | 18.0(3) | 5.35 |
| P3 | 1744.6(14) | 2667.1(12) | 5552.6(7) | 13.0(2) | 5.31 |
| P4 | 988.3(14) | 375.7(13) | 7072.1(7) | 12.6(3) | 5.33 |
| P5 | 6011.5(14) | 2992.0(13) | 8205.6(7) | 12.5(2) | 5.28 |
| P6 | 9147.5(14) | 5161.3(13) | 7965.9(7) | 12.5(3) | 5.27 |
| P7 | 8501.1(14) | 7514.4(13) | 9418.5(7) | 12.5(2) | 5.23 |
| P8 | 4401.9(14) | 7795.4(13) | 9716.2(7) | 13.8(2) | 5.40 |
| O1 | 6872(5) | 1850(4) | 2623(3) | 32.5(9) | 2.04 |
| O2 | 4417(5) | 3834(4) | 2970(3) | 32.1(9) | 2.08 |
| O3 | 7795(4) | 4195(4) | 3521(2) | 23.6(7) | 2.06 |
| O4 | 5850(5) | 2215(5) | 4256(2) | 31.5(9) | 2.09 |
| O5 | 7138(6) | 3816(5) | 5595(3) | 46.6(13) | 2.10 |
| O6 | 6220(6) | 983(5) | 5784(2) | 37.2(10) | 2.10 |
| O7 | 3884(5) | 3113(5) | 5579(3) | 35.6(9) | 2.13 |
| O8 | 1357(6) | 1538(4) | 4801(2) | 30.5(8) | 2.22 |
| O9 | 748(5) | 4163(4) | 5523(2) | 28.1(8) | 2.11 |
| O10 | 1456(6) | 1966(4) | 6572(2) | 33.9(9) | 2.02 |
| O11 | −1002(5) | −17(5) | 6919(3) | 29.1(8) | 2.11 |
| O12 | 1738(4) | 506(4) | 8053(2) | 19.6(6) | 2.18 |
| O13 | 6133(5) | 1678(4) | 7550(2) | 29.5(8) | 2.10 |
| O14 | 4640(4) | 4207(4) | 7956(3) | 26.6(8) | 2.08 |
| O15 | 8056(4) | 3692(4) | 8346(3) | 27.8(8) | 2.15 |
| O16 | 8790(5) | 5387(4) | 6943(2) | 21.9(7) | 2.20 |
| O17 | 8104(5) | 6532(4) | 8488(2) | 27.1(8) | 2.09 |
| O18 | 11095(4) | 4960(4) | 8334(2) | 19.1(7) | 2.19 |
| O19 | 9764(5) | 8781(4) | 9187(3) | 28.5(8) | 2.02 |
| O20 | 9049(5) | 6509(4) | 10224(2) | 25.4(7) | 2.21 |
| O21 | 6517(4) | 8272(4) | 9570(3) | 24.1(7) | 2.27 |
| O22 | 5623(5) | 2283(4) | 9210(2) | 28.6(8) | 2.15 |
| O23 | 3936(5) | 6382(4) | 9177(2) | 26.0(8) | 2.22 |
| O24 | 3321(4) | 9237(4) | 9583(2) | 24.1(7) | 2.06 |

Table S2. Selected bond distances (Å) and angles (deg) for (a) LiBePO4 and (b) BeP2O6.

(a) LiBePO4

| Atom‒Atom | Length/Å | Atom‒Atom | Length/Å |
| --- | --- | --- | --- |
| P1‒O8 | 1.532(1) | Be5‒O1 | 1.644(3) |
| P1‒O10 | 1.541(2) | Be5‒O17 | 1.627(3) |
| P1‒O15 | 1.530(2) | Be5‒O28 | 1.613(3) |
| P1‒O19 | 1.540(2) | Be5‒O8 | 1.606(3) |
| P2‒O1 | 1.541(2) | Be6‒O10#3 | 1.644(3) |
| P2‒O9 | 1.527(2) | Be6‒O14#13 | 1.626(3) |
| P2‒O23 | 1.532(1) | Be6‒O23 | 1.611(3) |
| P2‒O30 | 1.532(2) | Be6‒O25 | 1.637(3) |
| P3‒O2 | 1.542(2) | Be7‒O21#11 | 1.606(3) |
| P3‒O3 | 1.535(1) | Be7‒O31#4 | 1.634(3) |
| P3‒O28 | 1.534(1) | Be7‒O12 | 1.618(3) |
| P3‒O31 | 1.526(2) | Be7‒O16 | 1.628(3) |
| P4‒O12 | 1.539(1) | Be8‒O29#5 | 1.624(3) |
| P4‒O20 | 1.535(2) | Be8‒O27 | 1.638(3) |
| P4‒O22 | 1.529(1) | Be8‒O28 | 1.624(3) |
| P4‒O32 | 1.541(1) | Be8‒O32 | 1.606(3) |
| P5‒O4 | 1.534(1) | Li1‒O19#3 | 2.035(5) |
| P5‒O14 | 1.536(2) | Li1‒O25 | 2.028(4) |
| P5‒O18 | 1.541(1) | Li1‒O27 | 2.045(5) |
| P5‒O29 | 1.525(2) | Li1‒O3 | 2.014(4) |
| P6‒O11 | 1.535(1) | Li2‒O22#1 | 2.025(5) |
| P6‒O16 | 1.534(2) | Li2‒O30#11 | 2.062(5) |
| P6‒O17 | 1.530(2) | Li2‒O17 | 2.081(5) |
| P6‒O26 | 1.537(2) | Li2‒O4 | 2.065(4) |
| P7‒O5 | 1.529(1) | Li3‒O23#11 | 2.022(4) |
| P7‒O7 | 1.542(2) | Li3‒O16 | 2.027(4) |
| P7‒O21 | 1.538(1) | Li3‒O20 | 1.997(4) |
| P7‒O25 | 1.529(2) | Li3‒O28 | 2.056(5) |
| P8‒O6 | 1.535(1) | Li4‒O1#11 | 1.938(4) |
| P8‒O13 | 1.537(2) | Li4‒O6#12 | 2.047(4) |
| P8‒O24 | 1.542(2) | Li4‒O12#9 | 2.056(4) |
| P8‒O27 | 1.533(2) | Li4‒O15 | 1.947(4) |
| Be1#11‒O18 | 1.631(3) | Li5‒O8#3 | 2.134(5) |
| Be1‒O13 | 1.638(3) | Li5‒O13#3 | 2.037(4) |
| Be1‒O30 | 1.610(3) | Li5‒O14#13 | 1.993(5) |
| Be1‒O30 | 1.618(3) | Li5‒O18#13 | 2.648(4) |
| Be2‒O15#7 | 1.614(3) | Li6‒O10 | 1.924(4) |
| Be2‒O22#1 | 1.645(3) | Li6‒O7#9 | 2.070(4) |
| Be2‒O24#11 | 1.624(3) | Li6‒O9#1 | 1.956(4) |
| Be2‒O11 | 1.606(3) | Li6‒O11#10 | 2.031(4) |
| Be3‒O2 | 1.633(3) | Li7‒O2 | 1.917(4) |
| Be3‒O4 | 1.609(3) | Li7‒O29#3 | 1.977(4) |
| Be3‒O19 | 1.620(3) | Li7‒O21#14 | 1.978(4) |
| Be3‒O20 | 1.640(3) | Li7‒O24#14 | 2.086(4) |
| Be4‒O6 | 1.609(3) | Li8‒O18 | 1.925(5) |
| Be4‒O5#1 | 1.637(3) | Li8‒O26#12 | 2.112(4) |
| Be4‒O9#4 | 1.620(3) | Li8‒O31#11 | 1.956(4) |
| Be4‒O26 | 1.607(3) | Li8‒O32#12 | 2.009(4) |
| Atom‒Atom‒Atom | Angle/deg | Atom‒Atom‒Atom | Angle/deg |
| O8−P1−O10 | 107.83(8) | O15−P1−O8 | 110.45(8) |
| O15−P1−O10 | 108.57(8) | O29−P5−O14 | 110.76(8) |
| O15−P1−O19 | 109.93(9) | O29−P5−O18 | 109.06(8) |
| O9−P2−O1 | 109.09(8) | O11−P6−O26 | 106.18(8) |
| O9−P2−O23 | 110.13(8) | O16−P6−O11 | 114.46(8) |
| O9−P2−O30 | 110.3(9) | O16−P6−O26 | 106.75(8) |
| O23−P2−O1 | 108.7(8) | O17−P6−O11 | 108.58(8) |
| O23−P2−O30 | 109.43(8) | O17−P6−O16 | 107.4(9) |
| O30−P2−O1 | 109.17(8) | O17−P6−O26 | 113.62(9) |
| O3−P3−O2 | 109.01(8) | O5−P7−O7 | 108.09(8) |
| O28−P3−O2 | 107.67(8) | O5−P7−O21 | 113.39(8) |
| O28−P3−O3 | 110.18(8) | O21−P7−O7 | 107.14(8) |
| O31−P3−O3 | 109.94(9) | O25−P7−O5 | 108.53(8) |
| O4−P5−O18 | 108.7(8) | O25−P7−O7 | 109.57(8) |
| O29−P5−O4 | 109.7(8) |  |  |

Symmetry transformations used to generate equivalent atoms:

#1 +X, −1+Y, +Z; #2 −1/2+X, 1/2+Y, +Z; #3 +X, 1+Y, +Z; #4 +X, 1−Y, −1/2+Z; #5 −1/2+X, 1/2−Y, −1/2+Z; #6 1/2+X, −3/2+Y, +Z; #7 +X, −Y, −1/2+Z; #8 −1/2+X, 3/2−Y, −1/2+Z; #9 +X, 1−Y, 1/2+Z; #10 +X, −Y, 1/2+Z; #11 1/2+X, −1/2+Y, +Z; #12 1/2+X, 1/2−Y, 1/2+Z

(b) BeP2O6

| Atom‒Atom | Length/Å | Atom‒Atom | Length/Å |
| --- | --- | --- | --- |
| P1‒O3 | 1.568(3) | P6‒O17 | 1.597(3) |
| P1‒O2 | 1.440(3) | P7‒O21 | 1.577(3) |
| P1‒O1 | 1.483(4) | P7‒O19 | 1.460(3) |
| P1‒O4 | 1.575(3) | P7‒O17 | 1.567(3) |
| P2‒O4 | 1.567(3) | P7‒O20 | 1.457(3) |
| P2‒O7 | 1.568(3) | P8‒O24 | 1.461(4) |
| P2‒O5 | 1.434(4) | P8‒O23 | 1.457(4) |
| P2‒O6 | 1.472(4) | P8‒O21 | 1.581(3) |
| P3‒O9 | 1.465(4) | P8‒O22#1 | 1.578(3) |
| P3‒O10 | 1.584(4) | Be1‒O2 | 1.616(6) |
| P3‒O8 | 1.448(3) | Be1‒O11#4 | 1.606(6) |
| P3‒O7 | 1.561(3) | Be1‒O13 | 1.592(6) |
| P4‒O12 | 1.449(3) | Be1‒O22 | 1.616(7) |
| P4‒O11 | 1.451(3) | Be2‒O18#10 | 1.633(6) |
| P4‒O32 | 1.603(3) | Be2‒O14#2 | 1.612(6) |
| P4‒O10 | 1.583(4) | Be2‒O23#2 | 1.580(6) |
| P5‒O14 | 1.452(4) | Be2‒O1 | 1.579(6) |
| P5‒O15 | 1.568(3) | Be3‒O16#7 | 1.622(6) |
| P5‒O13 | 1.465(4) | Be3‒O8#12 | 1.592(6) |
| P5‒O22 | 1.582(3) | Be3‒O5#7 | 1.580(6) |
| P6‒O18 | 1.450(3) | Be3‒O9 | 1.615(6) |
| P6‒O16 | 1.458(3) | Be4‒O12#11 | 1.627(6) |
| P6‒O15 | 1.592(3) | Be4‒O19#7 | 1.591(6) |
| Atom‒Atom‒Atom | Angle/deg | Atom‒Atom‒Atom | Angle/deg |
| O3‒P1‒O4 | 103.2(2) | O19‒P7‒O21 | 106.8(2) |
| O2‒P1‒O3 | 111.2(2) | O14‒P5‒O15 | 110.6(2) |
| O2‒P1‒O1 | 118.2(2) | O14‒P5‒O13 | 118.0(2) |
| O2‒P1‒O4 | 108.5(2) | O14‒P5‒O22 | 109.7(2) |
| O1‒P1‒O3 | 106.3(2) | O15‒P5‒O22 | 104.5(2) |
| O1‒P1‒O4 | 108.5(2) | O13‒P5‒O15 | 106.3(2) |
| O4‒P2‒O7 | 107.3(2) | O13‒P5‒O22 | 106.8(2) |
| O5‒P2‒O4 | 109.8(2) | O18‒P6‒O16 | 117.6(2) |
| O5‒P2‒O7 | 104.9(2) | O18‒P6‒O15 | 104.9(2) |
| O5‒P2‒O6 | 121.6(3) | O18‒P6‒O17 | 112.4(2) |
| O6‒P2‒O4 | 104.0(2) | O16‒P6‒O15 | 112.6(2) |
| O6‒P2‒O7 | 108.6(2) | O16‒P6‒O17 | 107.7(2) |
| O9‒P3‒O10 | 105.4(2) | O15‒P6‒O17 | 100.2(2) |
| O9‒P3‒O7 | 104.5(2) | O19‒P7‒O17 | 106.9(2) |
| O8‒P3‒O9 | 120.0(2) | O17‒P7‒O21 | 103.0(2) |
| O8‒P3‒O10 | 112.3(2) | O20‒P7‒O21 | 109.3(2) |
| O8‒P3‒O7 | 108.4(2) | O20‒P7‒O19 | 118.8(2) |
| O7‒P3‒O10 | 105.0(2) | O20‒P7‒O17 | 110.8(2) |
| O12‒P4‒O11 | 116.5(2) | O24‒P8‒O21 | 104.9(2) |
| O12‒P4‒O3 | 111.8(2) | O24‒P8‒O22#1 | 108.5(2) |
| O12‒P4‒O10 | 106.5(2) | O23‒P8‒O24 | 122.8(2) |
| O11‒P4‒O3 | 109.1(2) | O23‒P8‒O21 | 109.3(2) |
| O11‒P4‒O10 | 111.5(2) | O23‒P8‒O22#1 | 104.5(2) |
| O10‒P4‒O3 | 100.2(2) | O22#1‒P8‒O21 | 105.8(2) |

Symmetry transformations used to generate equivalent atoms:

#1 −X, 1/2+Y, 2−Z; #2 1−X, −1/2+Y, 1−Z; #3 2−X, 1/2+Y, 1−Z; #4 1+X, +Y, +Z; #5 +X, −1+Y, +Z; #6 1−X, 1/2+Y, 1−Z; #7 −1+X, +Y, +Z; #8 1−X, −1/2+Y, 2−Z; #9 −X, −1/2+Y, 1−Z; #10 2−X, −1/2+Y, 1−Z; #11 +X, 1+Y, +Z; #12 −X, 1/2+Y, 1−Z

Table S3. Applicability of ionic potential modulation strategy in known alkali/alkaline-earth metal NLO materials.

| Compound | Ions | φ | SHG | Ref. |
| --- | --- | --- | --- | --- |
| α-KZnPO4 | K+ | 6.45 | 0.2 × KDP | 1 |
| α-LiZnPO4 | Li+ | 16.95 | 2.9 × KDP | 1 |
| K2SrP4O12 | Sr2+ | 15.87 | 0.5 × KDP | 2 |
| KMg(H2O)PO4 | Mg2+ | 27.78 | 1.14 × KDP | 3 |
| Ba3P3O10Cl | Ba2+ | 14.08 | 0.6 × KDP | 4 |
| Mg2PO4Cl | Mg2+ | 27.78 | 5.2 × KDP | 5 |
| Na2BeSiO4 | Na+ | 8.85 | 0.6 × KDP | 6 |
| Li2BeSiO4 | Li+ | 16.95 | 1.6 × KDP | 6 |
| Li2.9Cs1.1(SO4)2 | Cs+ | 5.52 | 0.3 × KDP | 7 |
| LiKSO4 | K+ | 7.25 | 1.2 × KDP | 8 |
| Li4Cs3B7O14 | Cs+ | 5.62 | 0.5 × KDP | 9 |
| Li4Sr(BO3)2 | Sr2+ | 15.87 | 2.0 × KDP | 10 |
| CsZn2B3O7 | Cs+ | 5.52 | 1.6 × KDP | 11 |
| Ba5Zn4(BO3)6 | Ba2+ | 14.08 | 2.5 × KDP | 12 |
| KNa4B2P3O13 | K+ | 6.62 | 0.4 × KDP | 13 |
| Na5B2P3O13 | Na+ | 8.62 | 1.0 × KDP | 14 |
| CsBPO4F | Cs+ | 5.32 | 0.3 × KDP | 15 |
| KBPO4F | K+ | 6.45 | 1.1 × KDP | 15 |
| RbCaCO3F | Rb+ | 5.92 | 1.11 × KDP | 16 |
| KCaCO3F | K+ | 7.25 | 3.61 × KDP | 16 |
| RbCaCO3F | Ca2+ | 18.19 | 1.11 × KDP | 16 |
| RbMgCO3F | Mg2+ | 35.09 | 4.0 × KDP | 17 |
| RbCd4Ga3S9 | Rb+ | 5.82 | 0.01 × AGS | 18 |
| KCd4Ga5S12 | K+ | 6.45 | 2.0 × AGS | 19 |
| Na2Hg3Sn2Se8 | Na+ | 8.85 | 5.4 × AGS | 20 |
| Li2HgSnSe4 | Li+ | 16.95 | 6.0 × AGS | 20 |

Figure S1. Crystal structure of Cs4LiBe4P7O24. (a) [LiBe4P7O24]∞ pseudo layers with twelve-membered rings. (b) 3D stacking of [LiBe4P7O24]∞ pseudo layers viewed along the a-axis.

Figure S2. Simulated and experimental powder XRD patterns of (a) LiBePO4 and BeP2O6.

(a) LiBePO4

(b) BeP2O6

Figure S3. XPS spectra of (a) LiBePO4 and (b) BeP2O6. LiBePO4: (a) XPS survey scan. (b)-(e) Fine XPS spectra of Li1s, Be 1s, P 2p, and O 1s, respectively. BeP2O6: (f) XPS survey scan. (g)-(i) Fine XPS spectra of Be 1s, P 2p, and O 1s, respectively.

Figure S4. TG and DSC curves of LiBePO4 and BeP2O6.

Figure S5. IR spectra of LiBePO4 and BeP2O6.

References

1.	X. M. He, L. Qi, W. Y. Zhang, R. X. Zhang, X. Y. Dong, J. H. Ma, M. Abudoureheman, Q. Jing and Z. H. Chen, Controlling the nonlinear optical behavior and structural transformation with a‐site cation in α‐AZnPO4 (A= Li, K), Small, 2023, 19, 2206991.

2.	Z. Y. Bai, L. H. Liu, L. Z. Zhang, Y. S. Huang, F. F. Yuan and Z. B. Lin, K2SrP4O12: A deep-UV transparent cyclophosphate as a nonlinear optical crystal, Chem. Commun., 2019, 55, 8454−8457.

3.	Z. Y. Bai, C.-L. Hu, L. H. Liu, L. Z. Zhang, Y. S. Huang, F. F. Yuan and Z. B. Lin, KMg(H2O)PO4: A Deep-Ultraviolet Transparent Nonlinear Optical Material Derived from KTiOPO4, Chem. Mater. , 2019, 31, 9540−9545.

4.	P. Yu, L.-M. Wu, L.-J. Zhou and L. Chen, Deep-Ultraviolet Nonlinear Optical Crystals: Ba3P3O10X (X = Cl, Br), J. Am. Chem. Soc. , 2013, 136, 480−487.

5.	J. X. Zhang, Q. G. Yue, S. H. Zhou, X. T. Wu, H. Lin and Q. L. Zhu, Screening Strategy Identifies an Overlooked Deep‐Ultraviolet Transparent Nonlinear Optical Crystal, Angew. Chem. Int. Ed., 2024, 63, e202413276.

6.	Y. ‐G. Chen, X. X. Jiang, H. ‐X. Lv, D. J. Mei, X. Zhang, Y. Guo, Z. S. Lin and X. ‐M. Zhang, Two α‐SiO2‐Related Deep‐Ultraviolet Phase‐Matchable Optical Nonlinear Beryllium Silicate Crystals Na2BeSiO4 and Li2BeSiO4 with Enhanced SHG Effect, Small, 2025, 21, 2408360.

7.	W. Yang, L. H. Liu, L. Z. Zhang, Y. S. Huang, F. F. Yuan and Z. B. Lin, Li2.9Cs1.1(SO4)2: An Ultraviolet Transparent Sulfate as a Nonlinear Optical Crystal, Cryst. Growth Des., 2023, 23, 5614−5620.

8.	P. F. Zhu, P. F. Gong, Z. Y. Wang, H. T. Jiang, J. F. Zhao, C. Li, Z. S. Lin, X. L. Duan and F. P. Yu, Enlargement of Bandgap and Birefringence in Nonlinear Optical Alkali-Metal Sulfate Crystals by the Substitution of Asymmetrical Non-π-Conjugated Cation, Adv. Optical Mater., 2023, 11, 2301152.

9.	Y. Yang, S. L. Pan, H. Y. Li, J. Han, Z. H. Chen, W. W. Zhao and Z. X. Zhou, Li4Cs3B7O14: Synthesis, Crystal Structure, and Optical Properties, Inorg. Chem., 2011, 50, 2415–2419.

10.	S. G. Zhao, P. F. Gong, L. Bai, X. Xu, S. Q. Zhang, Z. H. Sun, Z. S. Lin, M. C. Hong, C. T. Chen and J. H. Luo, Beryllium-free Li4Sr(BO3)2 for deep-ultraviolet nonlinear optical applications, Nat. Commun., 2014, 5, 1–5.

11.	A. H. Reshak, Novel borate CsZn2B3O7 single crystal with large efficient second harmonic generation in deep-ultraviolet spectral range, J. Alloys Compd., 2017, 722, 438-444.

12.	M. H. Duan, M. J. Xia and R. K. Li, Ba5Zn4(BO3)6: A Nonlinear-Optical Material with Reinforced Interlayer Connections and Large Second-Harmonic-Generation Response, Inorg. Chem., 2017, 56, 11458–11461.

13.	Y. Yang, P. F. Gong, Q. Huang, G. M. Song, X. M. Liu and Z. S. Lin, KNa4B2P3O13: A deep-ultraviolet transparent borophosphate exhibiting second-harmonic generation response, Inorg. Chem., 2019, 58, 8918-8921.

14.	Z. H. Li, Y. C. Wu, P. Z. Fu, S. L. Pan, G. F. Wang and C. T. Chen, Crystal growth of Na5 [B2P3O13], Chem. Lett., 2002, 31, 560-561.

15.	Q. R. Ding, S. G. Zhao, L. N. Li, Y. G. Shen, P. Shan, Z. Y. Wu, X. F. Li, Y. Q. Li, S. Liu and J. H. Luo, Abrupt structural transformation in asymmetric ABPO4F (A= K, Rb, Cs), Inorg. Chem., 2019, 58, 1733-1737.

16.	G. H. Zou, N. Ye, L. Huang and X. S. Lin, Alkaline-alkaline earth fluoride carbonate crystals ABCO3F (A= K, Rb, Cs; B= Ca, Sr, Ba) as nonlinear optical materials, J. Am. Chem. Soc., 2011, 133, 20001-20007.

17.	T. T. Tran, J. G. He, J. M. Rondinelli and P. S. Halasyamani, RbMgCO3F: a new beryllium-free deep-ultraviolet nonlinear optical material, J. Am. Chem. Soc., 2015, 137, 10504-10507.

18.	L.-Q. Yang, X.-M. Jiang, S.-M. Pei, W.-F. Chen, B.-W. Liu and G.-C. Guo, Optimizing the Nonlinear Optical Performance of an ANMQ (A: Alkali Metal; N: d¹⁰ Metal; M: Main Group Metal; Q: Chalcogen) System, ACS Appl. Mater. Interfaces., 2022, 14, 4352−4359.

19.	H. Lin, L.-J. Zhou and L. Chen, Sulfides with strong nonlinear optical activity and thermochromism: ACd4Ga5S12 (A= K, Rb, Cs), Chem. Mater., 2012, 24, 3406-3414.

20.	L. H. Gao, J. J. Xu, X. Y. Tian, B. B. Zhang, X. W. Wu and K. Wu, AgGaSe2-inspired nonlinear optical materials: tetrel selenides of alkali metals and mercury, Chem. Mater., 2022, 34, 5991-5998.